MATERIALS SCIENCE AND ENGINEERING

SEMINAR
Methods for Modifying Proton Exchange Membranes (PEM)

Using the Sol-Gel Process

by

Lisa C. Klein

Materials Science & Engineering

Rutgers University

Piscataway, NJ 08854

licklein@rci.rutgers.edu
ABSTRACT

NafionTM is commonly the membrane in PEM fuel cells.  To increase the operating temperature of PEMFC, inorganic nanoparticles have been introduced into NafionTM.  One route to inorganic nanoparticles is the sol-gel process, involving metal alkoxide hydrolysis and condensation.  NafionTM/sol-gel oxide hybrid membranes were prepared using an infiltration sol-gel process.  The inorganic content was controlled by the infiltration time.  Solvent uptake and swelling ratios were measured in distilled water and methanol solutions.  Fourier transform infrared (FT-IR) spectroscopy studies indicated that hybrid membranes have stronger absorptions from water and related species than unmodified Nafion membranes.  Hybrid membranes showed lower methanol uptake and lower swelling ratios than unmodified Nafion membranes.  Proton conductivities for hybrid membranes, compared to unmodified Nafion, decreased slightly with increasing infiltrated oxides.  Nevertheless, the decrease in proton conductivity was offset by a decrease in swelling.

DATE:
Friday, November 17, 2006

TIME:
3:30 PM – Refreshments


3:45 PM – Seminar

PLACE:
MSEE B012

Short Bio:

Lisa C. Klein obtained a BS in Metallurgy and a PhD in Ceramics from the Material Science and Engineering Department at the Massachusetts Institute of Technology.  With Rutgers since 1977, she became a full Professor in 1987.  She has been a visiting scientist at Sandia National Laboratory, Albuquerque, NM, at the University of Grenoble, Grenoble, France and Hebrew University of Jerusalem, Israel.  She is an Editor for the Journal of the American Ceramic Society.  Her areas of research are sol-gel processing of glasses, ceramics and organic-inorganic hybrids.  She served as a Member of the Functional Organic and Hybrid Materials Panel of the National Materials Advisory Board (NMAB) "Materials Research for 'Defense after Next'", and was Program Chair for the Spring 2003 Meeting of the Materials Research Society.






