MATERIALS ENGINEERING

SEMINAR
"Formation and Evolution of Tin Surface Defects During Cyclic Mechanical Loading"
By
Xi Chen
Purdue MSE Final Exam

Advisor: Professor Carol Handwerker and Professor John Blendell 

ABSTRACT

Sn surface defects are an issue in tin films and lead-free solders due to defects creating short circuits. Prior research has identified the mechanisms for surface defect evolution during aging and thermal cycling. The behavior of tin films due to mechanical stress, especially high frequency vibration is not fully understood. This research adds to the existing mechanisms for other thin films as well as puts forward new mechanisms. Piezoelectric drive of small atomic force microscopy (AFM) cantilevers vibrated at resonance are used for high frequency cyclic bending experiments. Intermetallic (IMC) formation as well as initial film morphology and thickness (corresponding to surface grain size) all influence the response of tin films for cyclic bending. A laser doppler vibrometer (LDV) system was used to identify the real-time strain along the cantilever during cycling, suggesting that the small strains are responsible for the limited nucleation and growth for defects though the defect density increases with the number of cycles and strain distribution along the cantilever. The effect of larger strains on defect evolution was determined using vibration of larger cantilevers at resonance as a function of number of cycles, frequency, temperature, and whether the vibration was continuous or interrupted for SEM characterization of defect type and density. In addition to typical micro-sized whiskers and hillocks, intragranular breakup (IGB) with intrusions and extrusions and nanowhiskers (NWs) with diameters < 1 [image: image2.png]


m were observed. Both increasing number of cycles and strain amplitude/rate promote defect formation for a fixed frequency, with the defect density being strongly frequency dependent. Vibration at low temperature and interrupting measurements for SEM characterization affected the relative densities. The density of micro-sized surface defects is strongly influenced by interruptions while NW density is almost unaffected. Both low resonant frequency and low T (223 K) promote IGB formation during cyclic bending due to large maximum strain amplitude and slower diffusion/creep at low T, respectively. Though the overall defect density for low T is smaller than that at room temperature (RT), the response of films is similar to that at RT, indicating the same mechanisms. The defect density decrease at low T is mainly determined by NW formation, and there is a transition from micro-sized surface defects to IGBs for cyclic bending at low T. This research demonstrated that cyclic bending of cantilevers can be used to quantify the stress relaxation of tin films in an important stress regime for microelectronics and to develop defect mitigation strategies to improve the reliability of interconnects in electronic applications.

Date: Thursday, June 4, 2020
Time: 2:00 PM
WebEx:  616 574 836
Meeting password: ebFED8c4Ra6
PURDUE MSE


[image: image3.png]



_914848933.doc
�



�
















