MATERIALS SCIENCE AND ENGINEERING

SEMINAR

“Impact Damage in Aircraft Composite Sandwich Panels”
by

Matthew Mordasky
Final Examination

Advisor
Wayne Chen

ABSTRACT

Composites become an attractive material for aircraft and rotorcraft which are commonly deployed in environments where man-made and naturally occurring material impacts can occur. An experimental study was conducted to develop an understanding of the damage caused by runway debris and environmental threats on aircraft structures. The velocities of impacts for stationary aircraft and aircraft under landing and takeoff speeds were investigated. The impact damage by concrete, asphalt, aluminum, hail and rubber sphere projectiles was explored in detail. Additionally, a kinetic energy and momentum experimental study was performed to look at the nature of the impacts in more detail. A method for recording the contact force history of the impact by an instrumented projectile was developed and tested. The sandwich composite investigated was an IM7-8552 unidirectional prepreg adhered to a NOMEX® core with an FM300K film adhesive. 

Impact experiments were conducted with a gas gun built in-house specifically for delivering projectiles to a sandwich composite target in this specific velocity regime (10-140 m/s). The effect on the impact damage by the projectile was investigated by ultrasonic C-scan, high speed camera and scanning electron and optical microscopy. Ultrasonic C-scans revealed the full extent of damage caused by each projectile, while the high speed camera enabled precise projectile velocity measurements that were used for striking velocity, kinetic energy and momentum analyses. Scanning electron and optical images revealed specific features of the panel failure and manufacturing artifacts within the lamina and honeycomb core. The damage of the projectiles was found to have a similar damage area for equivalent energy levels, except for rubber which had a damage area that increased greatly with striking velocity. 

Further investigation was taken by a kinetic energy and momentum based comparisons of 19 mm diameter stainless steel sphere projectiles in order to examine the dominating damage mechanisms. The sandwich targets were struck by acrylic, aluminum, alumina, stainless steel and tungsten carbide spheres of the same geometry and surface finish. A peak absorbed energy for perforation of 34.5J was identified regardless of the projectile density. The effect of composite panel manufacturing methods on the impact damage and energy absorption of the panel was also investigated. Specifically, damage related to pre-cured facesheets is compared to the co-cured facesheets used throughout the study.
Date:
Monday, November 28, 2011
Time:
2:30 P.M.
Place:
ARMS 1028
PURDUE MSE

    








_914848933.doc
�



�
















